Large-Scale Testing Setup (Pipe Preparation)

Dated

31st March 2023

Table of Contents

1	Preparation of the pipe	2

List of Figures

Figure 1: Flow chart for the preparation of the pipe	2

Figure 2: Picture of the steps taken for the preparation of the pipe	2

Figure 3: Dimensions of the pipe	6

Figure 4: Schematic of the pipe inside the container	6

List of Tables

Table 1: Initial measurement of the pipe	3

Table 2: OD measurement with vernier caliper at each point of radial section	3

Table 3: OD measurement with pi tape at each point of radial section	4

Table 4: Wall thickness each point of radial section	5

# Preparation of the pipe

Figure 1 and 2 shows the steps taken for the preparation of the 10 ¾” casing for testing. While table 1 to 4 shows the OD and thickness of the given pipe

Figure 1: Flow chart for the preparation of the pipe

Figure 2: Picture of the steps taken for the preparation of the pipe

Table 1: Initial measurement of the pipe

| Length (ft) | OD (mm) | ID (mm) |
| --- | --- | --- |
| 37.57 | 275.28 | 213.76 |

Table 2: OD measurement with vernier caliper at each point of radial section

| Section # | CALIPER (mm) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | OD (A-E) | OD (B-F) | OD (C-G) | OD (D-H) | AVERAGE (mm) |
| 1 | 276.20 | 275.86 | 275.94 | 275.92 | 275.98 |
| 2 | 275.93 | 275.57 | 275.52 | 275.62 | 275.66 |
| 3 | 276.05 | 275.60 | 275.49 | 275.70 | 275.71 |
| 4 | 275.97 | 275.78 | 275.64 | 275.60 | 275.75 |
| 5 | 275.97 | 275.85 | 275.50 | 275.51 | 275.71 |
| 6 | 275.92 | 275.95 | 275.50 | 275.42 | 275.70 |
| 7 | 275.89 | 275.88 | 275.46 | 275.41 | 275.66 |
| 8 | 275.80 | 275.91 | 275.71 | 275.48 | 275.73 |
| 9 | 275.82 | 275.92 | 275.41 | 275.56 | 275.68 |
| 10 | 276.14 | 275.97 | 275.33 | 275.45 | 275.72 |
| 11 | 276.14 | 275.90 | 275.33 | 275.48 | 275.71 |
| 12 | 275.77 | 276.00 | 275.69 | 275.73 | 275.80 |
| 13 | 275.88 | 275.60 | 275.48 | 275.57 | 275.63 |
| 14 | 275.87 | 275.76 | 275.35 | 275.50 | 275.62 |
| 15 | 275.90 | 275.98 | 275.18 | 275.35 | 275.60 |
| 16 | 275.64 | 275.93 | 275.60 | 275.16 | 275.58 |
| 17 | 275.59 | 275.58 | 275.38 | 275.51 | 275.52 |
| 18 | 275.60 | 275.56 | 275.33 | 275.19 | 275.42 |
| 19 | 275.93 | 275.90 | 275.25 | 275.40 | 275.62 |
| 20 | 275.63 | 275.89 | 275.38 | 275.17 | 275.52 |
| 21 | 275.61 | 275.48 | 275.21 | 275.22 | 275.38 |
| 22 | 275.78 | 275.93 | 275.51 | 275.12 | 275.59 |
| 23 | 275.75 | 275.89 | 275.20 | 275.31 | 275.54 |
| 24 | 275.39 | 275.67 | 275.46 | 275.07 | 275.40 |
| 25 | 275.63 | 275.55 | 275.49 | 275.07 | 275.44 |
| 26 | 275.26 | 275.50 | 275.27 | 275.18 | 275.30 |
| 27 | 275.75 | 276.00 | 275.06 | 275.15 | 275.49 |
| 28 | 275.47 | 275.40 | 275.31 | 275.20 | 275.35 |
| 29 | 275.71 | 275.88 | 275.26 | 275.43 | 275.57 |
| 30 | 275.71 | 275.63 | 275.27 | 275.31 | 275.48 |

Table 3: OD measurement with pi tape at each point of radial section

| Section # | PI TAPE (mm) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | D | E | F | G | H | W. AVERAGE (mm) |
| 1 | 276.17 | 275.62 | 275.62 | 276.05 | 275.87 | 276.07 | 276.07 | 276.07 | 275.94 |
| 2 | 275.74 | 275.92 | 275.79 | 275.62 | 275.77 | 275.62 | 275.84 | 275.97 | 275.78 |
| 3 | 275.89 | 275.62 | 275.62 | 276.05 | 275.84 | 275.62 | 275.74 | 276.05 | 275.80 |
| 4 | 276.05 | 275.97 | 275.62 | 276.56 | 276.78 | 275.95 | 276.05 | 275.95 | 276.11 |
| 5 | 275.62 | 275.84 | 275.62 | 275.95 | 275.97 | 276.12 | 276.12 | 276.05 | 275.91 |
| 6 | 276.15 | 276.07 | 275.89 | 276.02 | 276.00 | 275.64 | 276.07 | 275.87 | 275.96 |
| 7 | 275.97 | 276.02 | 275.62 | 275.92 | 275.79 | 275.92 | 275.95 | 276.02 | 275.90 |
| 8 | 275.87 | 276.05 | 275.95 | 275.89 | 275.92 | 276.15 | 276.07 | 275.95 | 275.98 |
| 9 | 275.84 | 275.89 | 275.74 | 275.92 | 276.02 | 275.95 | 275.97 | 275.87 | 275.90 |
| 10 | 275.87 | 276.05 | 275.87 | 276.05 | 276.05 | 276.05 | 276.12 | 276.07 | 276.02 |
| 11 | 276.00 | 275.97 | 276.15 | 275.89 | 276.17 | 276.15 | 276.05 | 275.84 | 276.03 |
| 12 | 276.05 | 275.95 | 276.10 | 275.84 | 275.95 | 275.95 | 276.15 | 275.87 | 275.98 |
| 13 | 276.05 | 275.84 | 276.15 | 275.82 | 275.84 | 275.62 | 275.84 | 275.77 | 275.87 |
| 14 | 275.95 | 275.77 | 275.84 | 275.92 | 275.92 | 275.62 | 275.77 | 276.00 | 275.85 |
| 15 | 275.87 | 275.87 | 275.84 | 276.05 | 275.77 | 275.97 | 276.05 | 275.95 | 275.92 |
| 16 | 275.95 | 275.64 | 275.97 | 275.84 | 275.95 | 275.84 | 275.87 | 275.95 | 275.88 |
| 17 | 276.12 | 275.92 | 275.97 | 276.00 | 275.67 | 275.64 | 275.74 | 275.72 | 275.85 |
| 18 | 275.74 | 276.07 | 275.72 | 275.72 | 275.72 | 275.72 | 275.84 | 275.74 | 275.78 |
| 19 | 275.74 | 275.87 | 275.97 | 275.89 | 275.82 | 275.72 | 275.72 | 275.72 | 275.81 |
| 20 | 275.72 | 275.62 | 275.62 | 275.69 | 275.84 | 275.87 | 275.62 | 275.62 | 275.70 |
| 21 | 275.62 | 275.87 | 276.23 | 276.20 | 276.20 | 276.15 | 275.62 | 275.97 | 275.98 |
| 22 | 275.97 | 275.64 | 275.72 | 275.72 | 276.10 | 276.23 | 275.62 | 275.67 | 275.83 |
| 23 | 275.74 | 276.10 | 275.74 | 275.92 | 275.64 | 275.62 | 275.72 | 275.84 | 275.79 |
| 24 | 275.64 | 275.72 | 275.67 | 275.72 | 275.84 | 275.84 | 276.17 | 275.72 | 275.79 |
| 25 | 275.62 | 275.64 | 275.69 | 275.62 | 275.64 | 275.64 | 275.62 | 275.69 | 275.64 |
| 26 | 275.72 | 275.56 | 275.51 | 275.62 | 275.82 | 275.62 | 275.62 | 275.77 | 275.65 |
| 27 | 275.62 | 275.54 | 275.56 | 275.01 | 275.01 | 275.54 | 275.62 | 275.62 | 275.44 |
| 28 | 275.62 | 275.64 | 275.62 | 275.62 | 275.84 | 275.64 | 275.62 | 275.64 | 275.65 |
| 29 | 275.97 | 275.82 | 275.62 | 275.74 | 275.62 | 275.77 | 275.77 | 275.97 | 275.78 |
| 30 | 275.44 | 275.34 | 276.05 | 275.56 | 275.62 | 275.62 | 275.77 | 275.95 | 275.67 |

Table 4: Wall thickness each point of radial section

| Section # | WALLTHICKNESS (mm) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | D | E | F | G | H | W. AVERAGE (mm) |
| 1 | 23.31 | 23.18 | 23.40 | 23.40 | 23.49 | 23.31 | 23.65 | 23.17 | 23.36 |
| 2 | 23.29 | 23.31 | 23.58 | 23.64 | 23.79 | 23.27 | 23.53 | 23.17 | 23.45 |
| 3 | 23.31 | 23.18 | 23.40 | 23.86 | 23.67 | 23.15 | 23.45 | 22.94 | 23.37 |
| 4 | 23.53 | 23.65 | 23.33 | 23.46 | 23.40 | 23.18 | 23.36 | 23.29 | 23.40 |
| 5 | 23.49 | 23.73 | 23.16 | 23.37 | 23.45 | 23.21 | 23.38 | 23.41 | 23.40 |
| 6 | 23.20 | 23.56 | 23.04 | 23.45 | 23.54 | 23.23 | 23.30 | 23.56 | 23.36 |
| 7 | 22.86 | 23.44 | 23.15 | 23.73 | 23.60 | 23.28 | 23.18 | 23.11 | 23.29 |
| 8 | 23.27 | 23.64 | 23.44 | 23.36 | 23.38 | 23.21 | 22.77 | 23.45 | 23.32 |
| 9 | 23.54 | 24.14 | 23.37 | 23.30 | 23.18 | 23.15 | 22.66 | 23.83 | 23.40 |
| 10 | 23.89 | 23.67 | 22.87 | 23.01 | 23.05 | 23.46 | 23.21 | 24.08 | 23.41 |
| 11 | 23.57 | 23.13 | 22.56 | 22.71 | 22.94 | 23.97 | 23.49 | 24.23 | 23.33 |
| 12 | 23.15 | 22.94 | 22.74 | 23.03 | 23.43 | 23.71 | 23.71 | 24.15 | 23.36 |
| 13 | 23.65 | 22.76 | 22.97 | 23.34 | 23.89 | 23.46 | 23.79 | 23.73 | 23.45 |
| 14 | 23.10 | 22.84 | 23.08 | 23.26 | 23.67 | 23.45 | 23.59 | 23.69 | 23.34 |
| 15 | 22.96 | 22.65 | 23.00 | 23.09 | 23.41 | 23.53 | 23.55 | 23.45 | 23.21 |
| 16 | 23.08 | 22.39 | 22.98 | 23.48 | 23.68 | 23.30 | 23.88 | 23.59 | 23.30 |
| 17 | 22.76 | 22.36 | 22.95 | 23.69 | 23.73 | 23.31 | 23.57 | 22.91 | 23.16 |
| 18 | 22.51 | 22.48 | 23.08 | 23.63 | 23.73 | 23.09 | 23.07 | 22.43 | 23.00 |
| 19 | 22.70 | 22.74 | 23.14 | 23.49 | 23.39 | 22.86 | 22.90 | 22.51 | 22.97 |
| 20 | 22.57 | 22.97 | 22.83 | 23.29 | 23.37 | 22.84 | 22.59 | 22.28 | 22.84 |
| 21 | 22.66 | 22.91 | 22.90 | 23.08 | 23.36 | 22.63 | 23.15 | 22.41 | 22.89 |
| 22 | 22.34 | 22.81 | 23.03 | 23.14 | 23.48 | 22.70 | 22.61 | 22.30 | 22.80 |
| 23 | 22.12 | 22.78 | 22.90 | 23.18 | 23.40 | 22.68 | 22.65 | 22.24 | 22.74 |
| 24 | 22.21 | 22.91 | 23.09 | 22.74 | 23.03 | 22.33 | 22.37 | 22.19 | 22.61 |
| 25 | 22.07 | 22.80 | 22.84 | 22.75 | 22.90 | 22.26 | 22.46 | 22.34 | 22.55 |
| 26 | 22.39 | 22.65 | 22.70 | 22.41 | 22.39 | 22.29 | 22.41 | 22.64 | 22.49 |
| 27 | 22.26 | 22.27 | 22.29 | 22.31 | 22.75 | 22.64 | 22.90 | 22.93 | 22.54 |
| 28 | 22.16 | 22.29 | 22.45 | 22.55 | 22.69 | 23.10 | 22.71 | 22.83 | 22.60 |
| 29 | 22.15 | 22.39 | 22.61 | 23.16 | 22.85 | 22.93 | 22.71 | 22.64 | 22.68 |
| 30 | 22.19 | 22.46 | 22.85 | 23.11 | 23.03 | 22.90 | 22.37 | 22.46 | 22.67 |

Figure 3: Dimensions of the pipe

Figure 4: Schematic of the pipe inside the container