## Slide 1: Numerical Modeling for Hydraulic Fracture Prediction on Fused Silica Surrogate Cylindrical Samples
Varun Gupta

## Slide 2
50.8 mm
16 mm
25.4 mm
3.2 mm
Geometry and Material Properties
Material: Fused Quartz
Assumptions:
Linear Elastic material behavior is assumed with the following properties:
  Young’s Modulus = 74 Gpa
  Poisson’s Ratio = 0.17
  Fracture Toughness = 0.65-0.70 MPa m0.5
Thermo-mechanical effects are not considered
Goal: To predict overpressures required to fracture an homogeneous pure (surrogate) material with known mechanical properties to compare these values to experimental overpressures obtained in our lab-scale stimulation system.

## Slide 3
Numerical Model: Loading and BCs
Fixed
Pext = 5000 psi
Pint =
6000-9000 psi
Modeled as an axisymmetric problem
Constant confining pressure of 5000 psi is applied
Internal pressure is applied incrementally
Quantity of interest: Fracture parameters near the corner
Objective is to determine the internal pressure which leads to fracture

## Slide 4
Number of elements: 44915
Number of nodes: 136066
Quadratic quadrilateral elements are used
Localized refinement performed close to the corner
Mesh Details and Stress distribution
Maximum in-plane principal stress at
Pint = 9000 psi

## Slide 5
Direction of crack extension
θ
Chart: Energy Release Rate at different crack extension angles
| 0.0 | 5.294117647058822 | 10.58823529411765 | 15.88235294117647 | 21.17647058823529 | 26.47058823529412 | 31.76470588235293 | 37.05882352941175 | 42.35294117647058 | 45.0 | 47.64705882352941 | 52.94117647058823 | 58.23529411764706 | 63.5294117647059 | 68.82352941176471 | 74.11764705882352 | 79.41176470588237 | 84.70588235294117 | 90.00000000000001
J-integral | 0.80976 | 0.93193 | 0.99294 | 1.0465 | 1.0919 | 1.129 | 1.1574 | 1.1767 | 1.187 | 1.1886 | 1.188 | 1.1798 | 1.1624 | 1.136 | 1.1008 | 1.0572 | 1.0054 | 0.94599 | 0.82725
Maximum energy release rate is attained at an angle of 45°, which is the angle of crack initiation

## Slide 6
Stress Intensity Factor vs Internal Pressure
Chart: Stress Intensity Factor
| 6000.0 | 7000.0 | 8000.0 | 9000.0
KI | 0.18657 | 0.38733 | 0.58871 | 0.79005
Given the fracture toughness of KIC = 0.7 Mpa m0.5 , at 5000 psi confining pressure the fracture is predicted at Pint ~ 8500 psi, i.e., overpressure = 3500psi

## Slide 7
Effect of Different Confining Pressure
Chart: Different Confining Pressure
| 1000.0 | 2000.0 | 3000.0 | 4000.0
5000 psi | 0.18657 | 0.38733 | 0.58871 | 0.79005
10000 psi | 0.17565 | 0.37315 | 0.57357 | 0.77465
20000 psi | 0.16929 | 0.3513 | 0.54728 | 0.74631
Confining pressure does not seem to have a significant role in the fracturing overpressure.

## Slide 8
Smoothed corner
R 0.1mm
Smoothing the corner out averts failure until much higher load
For example, introducing 0.1 mm fillet radius increases the fracture
overpressure to ~10,600 psi